基于4-（1-咪唑基）苯甲酸配体构筑的一个单一配体

和两个混和配体配位聚合物的结构与性质

李田田1   郑盛润*, 2

(1贵阳中医学院, 贵阳, 550002)

(2华南师范大学化学与环境学院, 广州, 510006)

附加材料

Table S1 Selected bond lengths [nm] and angles[°] for the complexes.a

| Complex 1 |
| --- |
| Cu(1)-N(1) | 0.198 7(4) | Cu(1)-N(3)#2 | 0.199 1(5) |
| Cu(1)-O(1)#1 | 0.198 7(4) | Cu(1)-O(3) | 0.200 6(4) |
| N(1)-Cu(1)-O(1)#1 | 167.55(17) | N(1)-Cu(1)-O(3) | 89.94(18) |
| N(1)-Cu(1)-N(3)#2 | 94.28(19) | O(1)#1-Cu(1)-O(3) | 89.09(17) |
| O(1)#1-Cu(1)-N(3)#2 | 90.07(18) | N(3)#2-Cu(1)-O(3) | 163.80(18) |
| Complex 2 |
| Cd(1)-N(3) | 0.229 9(7) | Cd(1)-O(1) | 0.242 0(6) |
| Cd(1)-N(1)#1 | 0.230 9(6) | Cd(1)-O(2) | 0.244 0(6) |
| Cd(1)-O(1W) | 0.234 7(7) | Cd(1)-O(4)#2 | 0.247 8(6) |
| Cd(1)-O(3)#2 | 0.238 0(5) | N(3)-Cd(1)-N(1)#1 | 176.8(2) |
| N(1)#1-Cd(1)-O(2) | 89.9(2) | N(3)-Cd(1)-O(1W) | 88.2(3) |
| O(1W)-Cd(1)-O(2) | 83.3(3) | N(1)#1-Cd(1)-O(1W) | 91.3(3) |
| O(3)#2-Cd(1)-O(2) | 171.1(2) | N(3)-Cd(1)-O(3)#2 | 86.6(2) |
| O(1)-Cd(1)-O(2) | 52.8(2) | N(1)#1-Cd(1)-O(3)#2 | 90.2(2) |
| N(3)-Cd(1)-O(4)#2 | 84.3(2) | O(1W)-Cd(1)-O(3)#2 | 87.8(3) |
| N(1)#1-Cd(1)-O(4)#2 | 94.1(3) | N(3)-Cd(1)-O(1) | 91.1(2) |
| O(1W)-Cd(1)-O(4)#2 | 140.5(2) | N(1)#1-Cd(1)-O(1) | 91.4(2) |
| O(3)#2-Cd(1)-O(4)#2 | 53.2(2) | O(1W)-Cd(1)-O(1) | 136.1(3) |
| O(1)-Cd(1)-O(4)#2 | 82.9(2) | O(3)#2-Cd(1)-O(1) | 136.0(2) |
| O(2)-Cd(1)-O(4)#2 | 135.7(2) | N(3)-Cd(1)-O(2) | 93.2(2) |
| Complex 3 |  |  |  |
| Cd(1)-O(6)#1 | 0.221 60(18) | Cd(2)-O(5)#1 | 0.219 09(18) |
| Cd(1)-N(2)#2 | 0.223 2(2) | Cd(2)-O(7) | 0.226 27(18) |
| Cd(1)-O(2)#3 | 0.230 28(17) | Cd(2)-O(7)#5 | 0.226 28(18) |
| Cd(1)-O(1) | 0.230 79(16) | Cd(2)-O(1)#5 | 0.237 16(17) |
| Cd(1)-O(8) | 0.232 0(2) | Cd(2)-O(1) | 0.237 16(17) |
| Cd(2)-O(5)#4 | 0.219 09(18) | O(6)#1-Cd(1)-N(2)#2 | 94.71(9) |
| O(5)#4-Cd(2)-O(7)#5 | 94.34(7) | O(6)#1-Cd(1)-O(2)#3 | 92.29(7) |
| O(5)#1-Cd(2)-O(7)#5 | 85.66(7) | N(2)#2-Cd(1)-O(2)#3 | 86.25(8) |
| O(7)-Cd(2)-O(7)#5 | 180 | O(6)#1-Cd(1)-O(1) | 97.48(7) |
| O(5)#4-Cd(2)-O(1)#5 | 85.60(7) | N(2)#2-Cd(1)-O(1) | 167.74(8) |
| O(5)#1-Cd(2)-O(1)#5 | 94.40(7) | O(2)#3-Cd(1)-O(1) | 91.99(6) |
| O(7)-Cd(2)-O(1)#5 | 95.42(7) | O(6)#1-Cd(1)-O(8) | 131.12(8) |
| O(7)#5-Cd(2)-O(1)#5 | 84.58(7) | N(2)#2-Cd(1)-O(8) | 82.14(9) |
| O(5)#4-Cd(2)-O(1) | 94.40(7) | O(2)#3-Cd(1)-O(8) | 135.66(7) |
| O(5)#1-Cd(2)-O(1) | 85.60(7) | O(1)-Cd(1)-O(8) | 90.75(7) |
| O(7)-Cd(2)-O(1) | 84.58(7) | O(5)#4-Cd(2)-O(5)#1 | 180 |
| O(7)#5-Cd(2)-O(1) | 95.42(7) | O(5)#4-Cd(2)-O(7) | 85.66(7) |
| O(1)#5-Cd(2)-O(1) | 180 | O(5)#1-Cd(2)-O(7) | 94.34(7) |
| aSymmetry transformations used to generate equivalentatoms: #1 x,-y-1/2,z-1/2, #2 x+1,-y+1/2,z+1/2, #3 x,-y-1/2,z+1/2 #4 x-1,-y+1/2,z-1/2 for compound 1; #1 x-y+2/3,-y+1/3,-z+1/3, #2 y+1,x,-z, #3 x-y-1/3,-y+1/3,-z+1/3, #4 y,x-1,-z for compound 2; #1 x+1,y,z, #2 x+1/2,-y+1/2,z+1/2, #3 -x+1,y,-z+5/2, #4 -x,-y+1,-z+2, #5 -x+1,-y+1,-z+2, #6 x-1,y,z, #7 x-1/2,-y+1/2,z-1/2 for compound 3. |

Fig. S1 The simulated X-ray powder diffraction patterns (lower) and the measured one (upper) of compound 1.

Fig. S2 The simulated X-ray powder diffraction patterns (lower) and the measured one (upper) of compound 2.

Fig. S3 The simulated X-ray powder diffraction patterns (lower) and the measured one (upper) of complex 3.