Release Mechanisms and Properties of pH-responsive Drug Nanocarriers

LI Xiang-Zi1, 2  HU Ping-Jing2  ZHU Zhen-Duo2  ZHU Guo-Xing1  SHEN Xiao-Ping*,1  WANG Min2 SUN Yu2  FENG De-Xiang2

(1School of Chemistry & Chemical Engineering, Jiangsu University, Zhenjiang, Jiangsu 212013, China)

(2School of Pharmacy, Anhui Provincial Engineering Research Center for Polysaccharide Drugs, Wannan Medical College, Wuhu, Anhui 241000, China)

表S1 pH响应纳米载体的药物负载

Table S1 Drug loading of pH-responsive nanocarriers

| Carrier |  | Drug | Stirring time/h | EE c /% | LE d /% | Ref. |
| --- | --- | --- | --- | --- | --- | --- |
| Content | Diameter/nm | Dose/mg |  | Content | Solvent | Concentration /(mg·mL-1) | Volume /mL | pH |  |  |  |  |
| FeSi@PBLA@mPEG | 245 ± 11 | 30 |  | DOX | DMSO | 0.6 | 10 | 7.4 | 48 | 69 | 12.3 | 21 |
| PEG/PEI@ Fe3O4 | ~20 | 160 |  | DOX | DMSO | 0.325 | 8 | — | 24 | 84.6 | — | 22 |
| Fe3O4/CTA | ~15 | 200 |  | DOX | DMF | 0.2 | 25 | 1 | 72 | 57.5 | 5.75 | 23 |
| MNP@D-PEG-H | 15 | 20 |  | DOX | Acetate buffer | 2 | 3 | 5.6 | 48 | — | — | 24 |
| MNP@SPHP | 19 | 30 |  | DOX | PBS | 0.883 | 12 | — | 24 | 72.6 | 32.7 | 28 |
| pH-MNs | ~112.5 | — |  | DOX | H2O | 0.24 | — | 7.4 | 6 | 74.9 | 13 | 31 |
| MSN-NH2 | 102~220 | 10 |  | UA | DMF | 1 | 10 | — | 24 | — | — | 33 |
| Micelles | 92~143 | 1 a |  | DOX | DMF/H2O | — | — | 7.4 | — | 25~44 | 3.7~6.6 | 35 |
| HMS@C18 | ~100 | 4; 2; 0.4 e |  | DOX | SBF | 5 | 0.04 | — | 24 | 82; 81; 77 f | 4.1; 8.1; 38.5 f | 36 |
| CLPN 1 | 45~60 | 20 |  | Prednisolone | DMSO/PBS | 0.227 | 22 | 7.4 | 15 | — | 38.9 | 41 |
| Fe3O4@mSiO2 | ~40 | 60 |  | DOX | ethanol | 1 | 3 | — | 12 | — | 2.07~2.74 | 42 |
| HEDO–Fe3O4 | 18~20 | — |  | BTZ | DMF | 2000 b |  | — | 24 | 60 | — | 44 |
| MCM-TAA-Fe3O4 | — | 200 |  | DXMS | ethanol | 10 | 10 | — | 24 | 10.2 | — | 47 |
| MMSN-PAA | 240 | 50 |  | DOX | PBS | 0.5 | 25 | 7.4 | 24 | — | — | 50 |
| PAA–MHAPNs | 100 | 15 |  | DOX | PBS | 0.3 | 100 | 7.4 | 48 | 76 | 3.3 | 51 |
| Fe3O4@PAMAM | 10~15 | 10 |  | DOX | H2O | 2 | 1 | — | 24 | 78 | — | 54 |
| Au NRs-MMSNEs | 300×180 | 5 |  | DOX | PBS | 0.5 | 6 | — | 24 | 30 | — | 56 |
| Fe@SiO2@PLL/AL | 420×110 | 20 |  | DOX | H2O | 10 | 2 | 5 | — | — | 13.5 | 58 |
| HS-SPION-COOH | 160 ± 20 | 1.4 a |  | DOX | H2O | 4 | — | — | 2 | 42.3 | 9.4 | 59 |
| Triblock copolypeptides | 200~300 | 1 |  | DOX | Ethanol/PBS | 2 | 1 | 7.4 | 4 | 52~68 | 12~21 | 62 |
| FPC-NCs | ~100 | 1 |  | DOX | PBS | 0.2 | 10 | 7.4 | 24 | — | — | 63 |
| LAP | 42.5±11 | 3~10 a |  | DEX | H2O | 2 | — | 3, 7, 13 | 24 | 72~80 | 12.1~13.3 | 64 |
| Fe3O4/Au@polymer | 50 | 10 |  | MTX | H2O | 2.5 | 2 | — | 12 | 74 | 37 | 66 |
| DTS@CS–PMAA | 80 | 90 |  | AMBA | PBS | 12 | — | 4 | 4 | 90 | — | 68 |
| MGC | 13 | — |  | DOX | — | — | — | 2, 3, 4, 5, 6, 7, 8 | 72 | 90.9 | — | 72 |
| Fe3O4@GO@mSiO2 | 2000 | 50 |  | GCB | H2O | 6.66 | 3 | — | 24 | 78.7 | 14.1 | 73 |
| Fe3O4@PG-CD | 230 | 120 |  | 5-FU | H2O | 166.7 | — | — | 72 | 83.4 | 46.4 | 76 |
| MSNs@CNPBA | 150 | 160 |  | DOX | DMF | 8.75 | 4 | — | 6 | 47.48 | 8.16 | 80 |
| FA-MNPs | 20~25 | 10 |  | DOX | — | 0.3 | 10 | — | 24 | 23 | — | 82 |
| MNPs | — | 100 |  | Cisplatin | H2O | 1.25 | 40 | — | 48 | 1~3 | 4.2~6.8 | 83 |
| MMSNs/ES | 500 | 206 |  | Ibuprofen | hexane | 100000 b | 10 | — | 4 | 26.91 | — | 84 |
| M-MSN/PMAA | 225±20 | 2 |  | DOX | PBS | 0.15625 | 6.4 | 7.4 | 24 | 95.1 | 32.3 | 86 |
| NHA80/15/5-CBA | 10~80 | 50 |  | PTX | Ethanol | 5 | — | — | 24 | 67.8 | 3.6 | 87 |
| (CS-MNP)-g-poly(AA)-g-en-β-CD | 115 | 100 |  | CUR | Acetate buffer | 75 | 50 | 2, 3, 4, 4.5, 5.5 | 24 | 35-88.8 | 25-80 | 93 |
| CS MNPs | 1-8 | 2.5 a |  | DOX | PBS | 0.15, 0.3, 0.4, 0.5, 0.6 | — | 6 | 24 | 81-99 | — | 96 |
| TPP(GA)/MCNs | 68.7 | 8 a |  | DOX | H2O | 0.2 | 25 | — | 24 | 77.6 | 71 | 97 |
| CMChitoCar beads | ~100 | 500 |  | Diclofenac | H2O | 500 | 20 | — | 24 | 42-55 | — | 99 |
| Mn0.9Zn0.1Fe2O4 | 25 | 50 |  | DOX | Chloroform | 1 | — | — | 4 | — | — | 100 |
| Fe3O4@mSiO2 | 63 | 15 |  | DOX | H2O | 0.5 | 10 | — | 48 | 93.6 | — | 101 |
| CS MNPs | 5~7 | — |  | Bortezomib | PBS | 0.5, 5, 10, 15, 20 b | — | 4.7, 6, 7.2 | 24 | ~28-100 | — | 103 |
| MSN@PHis | 150-170 | 1 a |  | DOX | H2O | 0.4 | — | 3 | ~12 | 35.9, 37 | — | 105 |
| PIA-PEG-FA-PHIS | 80 | 20 |  | DOX | DMSO | 2 | 2 | — | 4 | — | — | 106 |
| SPIONs@PEI-CPs | ~230 | 0.2~7.14 |  | DOX | PBS | 0.033 | — | — | — | — | — | 113 |
| AGIO@CaP-CD | 150 | 2 |  | DOX | H2O | 1.5 | 2.0 | 10 | 1 | 0.55±0.03 | — | 114 |
| HAPUN/MNs | — | 100 |  | Dtxl | Ethanol | 20 | 5 | — | 24 | — | — | 115 |
| Fe3O4@mSiO2 | ~80 | 50 |  | Ibuprofen | hexane | 30 | 10 | — | 24 | — | — | 116 |
| Ni-Na@CNFs | ~100 | 25 |  | DOX | PBS | — | — | 5, 7, 8, .9, 10 | 5 | ~38 | — | 118 |
| Fe3O4@graphene | 70 | 20 |  | DOX | PBS | ~0.167 | 30 | 7.4 | 12 | 88.3 | — | 121 |
| MSNs-ICP | ~100 | 20 |  | Ce6 | ethanol | 0.5 | 4 | — | 24 | — | 2.4 | 123 |
| Fe3O4/PANI@ mSiO2 | ~450 | 10 |  | DOX | PBS | 1 | 2 | — | 24 | 96.8 | — | 124 |
| HPFe3O4 | 18 | 4; 2; 0.4 e |  | DOX | H2O | 0.2 | 1 | — | 24 | 79.4; 72.3; 65.86 f | — | 126 |
| SiO2@Fe3O4@C | 120 | 5 |  | DOX | PBS | 1 | 10 | 7.4 | 24 | — | ~56 | 127 |
| MnOx-HMCNs | 300 | 10 |  | DOX | PBS | 0.3 | 20 | — | 24 | — | — | 128 |
| Zr-MOFs | ~20 | 3 |  | 5-Fu | H2O | 3300 b | 1 | — | 12 | — | — | 129 |
| Fe3O4@MSN@β-CD | ~90 | 100 |  | Rh6G | H2O | 1000 b | 1.0 | 9.8 | 24 | — | — | 130 |
| M-MSN-P(NIPAM-co-MAA) | 210 | 5 |  | DOX | H2O | 1.0 | 1.5 | 5.1, 6, 7.4, 8.1, 9, 10 | 24 | 2.9–91.3 | — | 133 |
| MSN-NH-N=C-PADs | ~120 | 200 |  | DOX | H2O+CH3OH | 0.6 | 50 | 5.5 | 24 | 31.8-38.2 | — | 134 |
| MS(M-3) | ~100 | 30 |  | DOX | Tris buffer | 1 | 3 | 7.4 | 24 | — | — | 135 |
| HMSN-SS-CS@PEG | 200~300 | 200 |  | DOX | H2O | 4 | 5 | 3.0 | 12 | — | 36.3 | 142 |
| FPA | 150 | 100~500 |  | DOX | PBS | — | — | 7.4 | 24 | 75 | 1.88 | 144 |
| FBP | 150 | 100~500 |  | DOX | PBS | — | — | 7.4 | 24 | 69 | 1.1.72 | 145 |
| Ac-bCDs | 185~250 | 50 |  | RAP | CH2Cl2/H2O | ~2.857 | 7 | — | 3 | > 90 | 26.4-28.3 | 147 |

a mg·mL-1; b µmol·L-1; c EE = Entrapment efficiency; d LE = Loading efficiency; e different carriers dose are separated by semicolon; f different EE or LE value conrresponding to carriers dose in the third column.

表S2 pH响应纳米载体的透析袋式释药

Table S2 Drug release of pH-responsive nanocarriers with dialysis bag

| Drug-Carriers | NMWC (Da) | Dose of the loaded carriers (mg) | Release medium with dialysis bag | Release efficiency at the corresponding outer pH f (% vs 24 h a) | Ref. |
| --- | --- | --- | --- | --- | --- |
|  |  |  | Inner volume(mL) | Outer volume(mL) | Replace volume (mL) | Different outer pH e |  |  |
| DOX-PMMNP | 12000-14000 | 20 | 4 | 40 | 6 | 5.5, 7.4 | 63, 32 | 20 |
| DOX -FeSi@PBLA@mPEG | 3500 | 20 | — | 10 | 3 | 5.8, 7.4 | ~38, 21 | 21 |
| DOX - PEG/PEI@ Fe3O4 | — | 10 | 3 | 6 | 3 | 4.5, 5.5, 7.4 | ~68, 65, 24 | 22 |
| Fe3O4/CTA/DOX/PEG | 3500 | 20 | 5 | 75 | 2 | 5.0, 7.4 | ~44, 4 | 23 |
| β-NaYF4:Gd3+/Tb3+@PEI–MPH–DOX | 3500 | — | 1 | 10 | 1 | 5.0, 7.4 | ~55, 40 | 27 |
| MNP@SPHP@DOX | 3500 | 10 | 3 | 25 | 2 | 5.0, 7.4 | ~65, 8 | 28 |
| DOX-HA-ADH | 6000 | — | — | 20 | 2 | 5.0, 6.0, 7.4 | 45, 35, 12 | 29 |
| DOX-RHD/pGL-3 | 1000 | 0.5 | 1 | 10 | — | 5.0, 7.4 | ~66, 28 | 30 |
| DOX-loaded pH-MN2/1 | — | 20 | 5 | 15 | 2 | 5.0, 6.8, 7.4 | ~80, 28, 12 b | 31 |
| MCS-CAA-DOX | — | — | — | 10 | — | — | ~82; 25 d | 32 |
| DOX-mPEG-b-(PCL-g-P(DA-co-DMAEMA) | 3500 | 5 | 5 | 25 | — | 5.0, 6.5, 7.4 | 88, 59, 6 b | 35 |
| DOX -Fe3O4@mSiO2@P2 | 8000 | — | 5 | 20 | — | 5.8, 7.4 | ~95, 44 | 42 |
| MMSN-PAA | 3500 | 5 | 2 | 8 | 3 | 5.2, 6.3, 7.4 | ~13, 9.5, 0.5 | 50 |
| DOX-PAA–MHAPNs | 8000 | 3.0 | 10 | 100 | 1 | 5.0, 6.5, 7.4 | 72, 48, 15 | 51 |
| Pt@PAA-MSNDOX | 3500 | 10 | 5 | 50 | 5 | 5.5, 7.4 | ~19, 39; 2, 2 d | 52 |
| DOX-polymer@Fe3O4@PAMAM | — | 5 | 0.5 | 5 | 3 | 5.5, 7.4 | 75, 30 | 54 |
| DOX@MTX@nanogles | 10000 | 30 | 2 | 6 | 6 | 4.0, 5.5, 7.4 | 2, 2, 0; 23, 2, 2 d | 55 |
| DOX-Au NRs-MMSNEs | 8000 | 4 | — | 20 | 3 | 5.5, 7.4 | 50, 5 c | 56 |
| Dox-HS-SPION-COOH | 3500 | — | 4 | 6 | 1 | 5.0, 7.4 | ~58, 28 | 59 |
| DOX-B6-SA-NPs | 12000 | 2 | 1 | 100 | 0.2 | 5.8, 6.5, 7.4 | 80, 28 | 61 |
| DOX-triblock copolypeptides | — | — | 1 | 20 | 20 | 5.5, 7.4 | ~52, 38 | 62 |
| DOX -FPC-NCs | — | — | 5 | 50 | — | 5.0, 6.2, 7.4 | 43, 32, 22 | 63 |
| DEX -LD-NPs | 14000 | 6 | 2 | 8 | 1 | 5.4, 7.4 | ~81, 45 | 64 |
| MTX-Fe3O4/Au@polymer | 12000 | 5 | 1 | 25 | 3 | 5.3, 7.4 | 64, 42 | 66 |
| DOX-poly(NIPAAm-co-AA)/Fe3O4 | 3500 | 3 | 3 | 30 | 3 | 5.3, 7.4 | 52, 44 | 69 |
| GCB-Fe3O4@GO@mSiO2 | — | 5 | 0.5 | 5 | 3 | 5.5, 7.4 | 79, 30 | 73 |
| DOX -GO-ADH-Hep | 14000 | 0.5 | 1 | 20 | 1 | 5.0, 7.4 | ~30, 22.5 | 74 |
| PPT-CS-NPs | 7000 | 10 | — | 50 | — | 3.7, 6.8, 7.4 | 78, 61, 45 | 77 |
| MSNs@FITC@DOX | 1000 | — | 3 | 50 | 2 | 5.3, 6.8, 7.4 | ~71, 19, 8 | 80 |
| DOX-M-MSN/PMAA-10 | 14000 | — | 2 | 200 | 2 | 5.5, 7.4 | 39, 15.3 | 86 |
| DOX -SMGO/P(NIPAM-co-AA) | — | 10 | — | 80 | — | 5, 7 | ~47, 9 | 88 |
| DOX-TPP/MCNs | 12000 | 2 | — | 15 | 1 | 5.3, 7.4 | 34, 19 | 97 |
| DOX -CS/Fe3O4@mSiO2 | — | — | — | 6 | 3 | 4.0, 5.8, 7.5 | ~84, 70, 25 | 101 |
| DOX-PIA-PEG-PHIS-DNP | 3500 | — | 4 | 30 | 3 | 5.0, 5.7, 6.5, 7.0, 7.4 | ~84, 44, 33, 20, 4 | 106 |
| DOX-AGIO@CaP-CD | 3000 | — | 2 | 8 | — | — | ~100; 15.3 d | 114 |
| DOX -Fe3O4/PANI/mSiO2 | <15000 | 12 |  | — | — | 5.5, 6.5, 7.4 | ~88, 59, 6 b | 124 |
| DOX-SiO2@Fe3O4@C | 3500 | 5 | 10 | 15 | 15 | 5.0, 6.2, 7.4 | ~20, 12.5, 5 | 127 |
| DOX -MnOx-HMCNs | 5000 | 3.0 | — | 30 |  | 4.6, 6.0, 7.4 | ~40, 27.5, 20 | 128 |
| 5-Fu-Zr-MOFs | — | 1 | — | 3 | — | 2.0, 4.0, 5.0, 7.4 | 58, 43, 18, 4 | 129 |
| DOX-P(M-MSN-NIPAM-co-MAA) | 14000 | — | 2 | 200 | 1 | 5.0, 6.5, 7.4 | 80.2, 37.1, 7.2 | 133 |
| DOX-MSN-NH-N=C-PAD10 | — | 10 | 5 | 25 | 5 | 5.5, 6.0, 7.4 | ~73, 44, 7 | 134 |
| DOX-MS@S-NPs | 8000 | — | — | 5 | — | 2.0, 5.0, 7.4 | 89, 55, 2 b | 135 |
| DOX-FPA | 12000 | 1.5 | 1.5 | 30 |  | 5.5, 6.5, 7.4 | ~58, 23, 14 | 144 |
| DOX-FBP | 12000 | 1.5 | 1.5 | 30 |  | 5.5, 6.5, 7.4 | ~53, 20, 5 | 145 |
| RAP-Ac-bCDs(2.5-240) | 3500 | 5 | 0.2 | 10 | 4 | 7.4 | ~10-70 | 147 |

a Incubate time, and only 24 hours of release efficiency values are given; b vs 12 h; c vs 20 h; d two kinds of drugs loaded on the carrier at the same time, and the later group data are the release efficiency of the second drug at the corresponding pH; e different pH value are separated by comma; f different release efficiency data are separated by comma.

表S3 pH响应纳米载体的体外细胞毒性及荷药后抗肿瘤细胞效果

Table S3 Cytotoxicity and antitumor efficacy in vitor of pH-responsive nanocarriers

| Carriers | Cell line | Carrier concentration (µg mL-1) | Cell viability % vs carriers concentration (µg mL-1), 24 h a | Drug concentration loaded on nanocarriers (µg mL-1) | IC50 (µg mL-1) vs 24 h a | Ref. |
| --- | --- | --- | --- | --- | --- | --- |
| Fe3O4–NH2 | MCF-7 | — | — | DOX/— | 0.11 | 18 |
| PMMNP | MDA-MB-231 | — | — | DOX/0.03, 0.3, 3, 30 | ~3 c | 20 |
| FeSi@PBLA@mPEG-1 | NIH/3T3 | 10, 50, 100, 200 | >100 vs 200 c | — | — | 21 |
| Fe3O4/CTA/DOX/PEG | NIH/3T3 | 50, 200,400, 600,800, 1000 | ~90 vs 1000 | DOX/1.75, 3.5, 5, 7, 10, 15, 20 | ~20 f | 23 |
| PEI-β-NaYF4:Gd3+/Tb3+ | NIH 3T3 | 3.12, 6.25, 12.5, 25, 50, 100, 200 | ~96 vs 300 | — | — | 27 |
| MNP@SPHP | Hela | 1, 5, 10, 25, 50 | ~90 vs 50 | — | — | 28 |
| Lf-HA | C6 | 10, 20, 40, 60, 80, 100 | >99 vs 100 | DOX/0.5, 1, 2.5, 5, 10 | ~10 | 29 |
| pH-MN2/1 | Hela/COS-7 | 0.3, 1.2, 2.5, 5, 10, 30, 60 | >99 vs 100c | DOX/0.125, 0.25, 0.5, 1, 3, 6 | 0.7/3.1 c | 31 |
| MCS | Hela | 5, 10,30, 50, 80, 100 | 89 vs 100 e | DOX/0.5, 2, 4, 8, 10 | ~5.1 e | 32 |
| MSN-NH2 | HepG2 | 1, 25, 50, 100, 150, 200 | ~94 vs 200 | UA/1, 5, 10, 20, 30, 40 | ~17 | 33 |
| micelles | MCF-7; 4T1 h | 1, 10, 25, 50, 100, 250, 500, 1000 | >85 vs 1 | DOX/0.1,0.25,0.5,1,2.5,5,10 | ~2.5; 2.1 j | 35 |
| HMS@C18@SPIONPs | KB | 2.5, 5, 10, 25, 50, 100 | >80 vs 100 | — | — | 36 |
| SBAPF | HeLa | 5, 10, 20, 50, 100, 200 | >80 vs 200 | DOX/0.57, 1.14, 2.27, 5.68, 11.36, 22.72 | >5.68 | 37 |
| Fe3O4@mSiO2@P2-4000-3 | Hela | 3.125, 6.25, 12.5, 25, 50 | 88.3 vs 50 | — | — | 42 |
| HEDO–Fe3O4 | NIH3T3 | 0.01-100 | >98 vs 100 | — | — | 44 |
| MCM-TAA-Fe3O4 | MC3T3-E1 | 100 | 96 vs 100 | — | — | 47 |
| MMSN-PAA | HeLa | 10, 30, 50, 100 | >90 vs 100 | DOX/0.1, 1, 2, 5 | >5.0 | 50 |
| PAA–MHAPNs | HepG2 | 1, 10, 20, 40, 80, 160, 320 | ~80 vs 320 | DOX/5, 10, 15 | — | 51 |
| PAA-MSN | HeLa | 10, 50, 100, 250, 500 | ~90 vs 500 | DOX/0.01, 0.1, 1, 5, 10 | 0.208 | 52 |
| NIPAAm-MAA-DMAEMAQ | MCF-7 | 7.5, 15, 30, 60 | ~95 vs 60 d | — | — | 55 |
| Au NRs-MMSNE | MCF-7 | 40, 60, 80 | ~29 vs 80 (light) | — | — | 56 |
| Fe@SiO2@ AL/PLL | MCF-7 | 50, 100, 250, 500, 1000 | ~92 vs 1000 | DOX/0.09, 0.18, 0.46, 4.6, 46 b | ~0.46 b c | 58 |
| B6-SA-NPs | MDA-MB 231; LA7 h | — | — | 0.1, 0.5, 2, 10, 40 | 3.68; 1.61 j | 61 |
| Triblock copolypeptides | CT26 | 0.01, 0.1, 1, 10, 100 | > 94 vs 100 | DOX/0.1, 1.0, 10 | < 1.0 | 62 |
| FPC-NCs | DU145 | 50, 100, 150 | ~96 vs 150 | — | — | 63 |
| Fe3O4/Au@polymer | MCF7 | 0.01, 0.1, 1, 10, 100 | ~88 vs 100 | — | — | 66 |
| poly(NIPAAm-co-AA)/Fe3O4 | Hela | — | — | DOX/10, 15, 30, 40, 50 | 34 c | 69 |
| MGNs | Chang liver | 5, 10, 20, 40, 80 | 98 vs 80 | — | — | 71 |
| MGC | MCF-7 | 1, 2, 5, 10, 20 | ~91 vs 20 | DOX/1, 2, 5, 10, 20 | ~6 | 72 |
| PEG-dendritic NPs | A431 | 1000 | ~95 vs1000 | — | — | 73 |
| GO-ADH-Hep | HepG2; MCF-7 h | 0.01, 0.1, 1, 10, 100 | >90 vs 100 | DOX/0.01, 0.1, 1, 5, 10, 50 | ~50; 1.0 j | 74 |
| MSNs@FITC | HeLa; HepG2 h | 0.16, 0.32, 0.63, 1.25, 2.5, 5, 10 | >95 vs10 | — | — | 80 |
| FA-MNPs | Hela | 2.5, 5, 10, 15, 25, 50, 100 | ~97; 98 i vs 100 | DOX/— | 10 | 82 |
| PTX-NHA80/15/5-CBA | HeLa; MCF-7; T47D h | 5, 10, 15, 20, 25, 30, 35 b | 95; 75; 82 i vs 35 b | — | — | 87 |
| SMGO\P(NIPAM,-co-AA) | Hela | 20, 80, 170, 250, 340, 400 | >95 vs 410 | — | — | 88 |
| CS MNPs | MCF-7 | — | — | — | 1.0 b c | 96 |
| CS/Fe3O4@mSiO2 | HepG2 | 10, 20, 40, 60, 60, 100, 120 | >87 vs 120 | DOX/2.93, 5.86, 11.7, 17.6, 23.4, 29.3, 35.2 | ~23 | 101 |
| PIA-PEG-FA-PHIS | HeLa | 10, 25, 50, 100 | ~93 vs 100 | DOX/0.1, 1, 10 | — | 106 |
| SPIONs@PEI-CPs | A549; HepG2 h | 10, 20, 30, 40, 50, 60 | ~92; 95 i vs 60 | DOX/0.25, 0.5, 0.75, 1, 5 | 1; 0.9 j | 113 |
| AGIO@CaP-CD | SKBr3 | — | IC50 = 0.8 | — | 0.15 | 114 |
| HAPUN/MNs | SGC-7901 | 1, 10, 50, 100 | ~80 vs 100 | — | — | 115 |
| Ni-Na@CNFs | Hela | 3.0, 1.5, 0.75 | >100 vs 3 d | DOX/3.0, 1.5, 0.75 | — | 118 |
| Fe3O4@graphene | rat myocardial cells | 0.25-100 | ~98.52 vs 100 | — | — | 121 |
| SiO2@Fe3O4@C | MCF-7 | 3.9, 7.8, 15.6, 31.2, 62.5, 125, 500, 1000 | ~80 vs 1000 | — | — | 127 |
| MnOx-HMCNs | MDA-MB-231 | 2.5, 5, 10, 20 | >96 vs 20 | DOX/1.25, 2.5, 5, 10, 15, 20, 30 g | ~5.6 | 128 |
| Zr-MOFs | 293 | 3.125, 6.25, 12.5, 25, 50 | 96 vs 50 | — | — | 129 |
| Fe3O4@MSN@β-CD | HEK293T | 3.125, 6.25, 12.5, 25, 50, 100 | ~70 vs 100 c | — | — | 130 |
| M-MSN-P(NIPAM-co-MAA) | HeLa | 0.1, 1, 10, 100, 500 | ~96 vs 500 c | DOX/1.0 | 0.09 c | 133 |
| MSN-NH-N=C-PADs | HeLa | 3.2,6.3,12.5,25,50,100 | >75 vs 100 c | DOX/0.32, 0.63, 1.25, 2.5, 5.0, 10 | 0.63-1.25 c | 134 |
| MS@S-NPs | Hela | 3.125, 6.25, 12.5, 25, 50 | ~99 vs 50 c | — | — | 135 |
| Ni@Au | Molt-4 | 0.1, 1, 10, 100, 250, 500, 1000 | >90 vs 100 | — | — | 138 |
| HMSN-SS-CS@PEG | MCF-7 | 0.1, 1, 10, 100, 500 | ~80 vs 500 c | — | — | 142 |
| PP75-coated-liposomes | Hela | 7.5, 10, 15, 20, 25, 30, 37.5, 60, 300 | ~97 vs 300 | DOX/0.01, 0.05, 0.1, 0.25, 0.5, 1, 2.5, 5, 10 | ~0.86 b | 143 |
| FPA | KB | — | — | DOX/1, 2, 3, 4, 5, 6, 7 | 2.3c | 144 |
| FBP | KB | — | — | DOX/0.3125, 0.625, 1.25, 2.5, 5 | 0.49c | 145 |

a Incubate time; b µmol L-1; c 48 h; d 72 h; e 12 h; f 15 min; g vs MCF-7/ADR; h the different cell line name are separated by semicolon; i different group viability value conrresponding to cell line in the second column; j different IC50 value conrresponding to cell line at second column.